TECHNICAL DATA SHEET

## PTFE-Spray

## LOS 210

LOS 210 is a strongly adhering lubricant and separating agent without any grease.

For the application at conveyors, hinges, carriage rails, etc.

Use:

Shake the aerosol can vigorously before use.

Spray LOS 210 thinly from a distance of approx. 30cm. After spraying there will be a dry separating and gliding film, which is dirt- and water-repellent. Remove oil, dirt and grease from surfaces.

Technical Data:

Form:				Aerosol

Colour:			whitish

Odour:				like Petrol

Density (20°C):		0.59 g/cm³

Flash point:			<-60°C (Propellant)

Temperature resistance:	-50°C bis +260°C (short-term)

Solubility:			not water-soluble

Water hazard class:		WGK 1 (self-classification)

Packaging:			400 ml aerosol can (15 pc.)

Suggestions, processing and use of our products correspond to the best knowledge at printing of this leaflet and are always given without obligation. You only can serve as a clue in consideration of the changing conditions; from this no liabilities, liability and guarantee claims can be derived. Own tests must be carried out before application. Every manufacturer of our products is liable for the retention everything legal to regulations.

EURO-LOCK Vertriebs-GmbH* Nordweststr. 3 * 59387 Ascheberg * Tel. 02593/95887-0 * Telefax 02593/95887-29